## Slide 1
A Review of Typical Issues and Solutions of Motorcycle Battery production
January, 2019

## Slide 2
1
1
2
Contents
Jinkeli briefing
Typical issues of Mc battery production

## Slide 3
1
Typical Issues & Solutions of Mc Battery Production

## Slide 4
1.1 OCV Rapid Drop When Battery is in Placement

## Slide 5
Causes Analysis( Battery Self-discharge)
① High impurities of raw materials especially in acid, DM water, alloy and separators.
② Sulfate corrosives stick to the paste surface or AM
③ Oxides stick to the paste surface and comes into the battery
④ High Cl- and Fe3+ because of negative plates of dry-charged battery washed by recycled water made by neutralizing acid with NaOH.
⑤ Self-discharge due to ion conduction between the individual cells caused by the failure of the seal during the battery assembly process.

## Slide 7
Solutions( Reduce Battery Self-discharge)
① Ensure the high quality of raw materials source
② Regularly clean, maintain the equipment and replace toolings and molds
③ Use DM water to wash plates or even drop this process
④ Strength the running equipment parameter consistency during the battery assemble and inspection of process quality compliance

## Slide 8
1.2 Low Storage Performance of Dry-charged Mc Battery

## Slide 9
Causes Analysis
① Thermal passivation caused by positive plates exposure to high temperature and humidity for long time during drying
② High moisture of both positive and negative plates plus AGM separators(＞0.5%）
③ Negative AM-lead surface get oxidized resulting in low OCV after acid filling

## Slide 10
Solutions
① Try to use flush drying for positive plates
② Try to control the moisture of positive, negative and separators below 0.5%
③ Maintain same density and dipping time for negative plate, and keep some space between each plates
④Dipping tank shall be made of PP materials or glass fiber reinforced plastic material instead of stainless steel, in case of corrosives produced.

## Slide 11
1.3 Rapid Capacity Loss of AGM VRLA Mc Battery During Use

## Slide 12
Causes Analysis
① Grid alloy and lead paste formula not proper/suitable
② PAM/NAM ratio in per cell not proper
③ Bad curing performance
④ Poor stability of battery charger result in insufficient charged

## Slide 13
Solutions
① Positive gird Pb-Ca alloy parameter: Sn＞0.7%, Ca＜0.09%.
②Increase amount of Barium sulfate, reduce lignin dosage properly
③ Maintain PAM/NAM ratio in a proper range
④ Maintain a good curing effect ( A good-structure curing chamber and curing process)
⑤ Battery charger shall be suitable for battery.

## Slide 14
1.4 Plate Abnormal Corrosion as well as Frame & Ribs Fracture
at Early Stage

## Slide 15
Causes Analysis
① Grid alloy composition wrong mixture
② Temperature control issue during the grid making
③ Air holes generated in grid and ribs because of poor venting of mold or too much mold coat sprayed
④ Impurities remained during the alloy preparation

## Slide 16
Solutions
① Strictly control the alloy quality( specify the impurities and lead slag range)
② Set up a clear separation procedure during the alloy preparation
③ Set a reasonable temperature range of grid casting, regularly inspect and calibrate the temperature control system of grid casting machine
④ A proper venting structure design of mold

## Slide 17
2
Jinkeli Briefing

## Slide 18
Zibo, China
Henan, China
Hubei, China
Hochiminh, Vietnam
Jinkeli Location

## Slide 19
2
Today
※ Advanced battery R&D Center, continuous technical support and product development
※ The largest battery additives supplier in China and over 70% domestic market share
※ Global sales and service networks
※ ISO 9001:2008 & ISO14000&18000 , IATF16949
※ More than 180 employees
※ 53,334m² production and storage area
※ USD 9.2 million register capitals
※ Sales revenue of Year 2018 USD 50 million

## Slide 21
Lignin
(Vanisperse)
Humic acid
Pre-blended expander
Carbon black
Graphite
CuringBon®
（4BS seed）
Barium sulfate
Stannous Sulfate
Antimony Trioxide
Nano-silica Sol
Fiber Flock
Cork Powder/
Mold coat
Fumed Silica
KL-99 Anti-oxidation Oil
Seamless Pasting Belt
Products

## Slide 22
MAIN CUSTOMERS

## Slide 23
MAIN CUSTOMERS

## Slide 24
Jinkeli R&D Center was founded in 2007, and it consists of process lab, cell testing lab and battery testing lab as well as materials analysis labs, which are equipped with most advanced testing and experimental equipments. This enables us to develop the leading battery additives, advanced formula as well as the periodical battery tests of the products.
Besides, the center has worked closely with CBI, and the project was sponsored by them. We also work closely with Bulgaria Academy of Sciences, Borregaard, Cabot and other universities and institutions, We aim to be a globally leading providing complete solutions for battery additives.
R&D Center

## Slide 26
Technical & Engineering Team

## Slide 27
Labs & Equipments
Materials Analysis Lab Materials Analysis Lab High-temperature Lab

## Slide 28
Lab Equipments
Simultaneous thermal analyzer(DSC/TGA) Nano Laser particle size analyzer Electrochemical workstation
Atomic absorption spectrometer SEM XRD

## Slide 29
Labs & Equipments-process lab
Paste mixing
Pasting
Plates pressing
Curing
COS
Assembly
Batteries
Mixing

## Slide 30
Labs- Cell & Battery Testing Lab

## Slide 31
Cycle life test ,
Over-charge and over-discharge rate test ,
Capacity test ,
Internal resistance test ,
Charge retention test ,
Battery performance under different temperature ,
Etc.
Accuracy up to 0.02%
Temperature range: -60℃~150℃
Totally 400 testing circuits

## Slide 32
Thanks for your attention.
Welcome to visit our booth
No. 144.